## Slide 1
Supervisor
Dr. Pradeep Kumar
Nasaru Khan
(D20066)
PhD Research Scholar
School of Physical Sciences
Indian Institute of Technology Mandi
IPS Meeting 2025-Singapore

## Slide 2
No true long range order
Power low decay of correlation functions
Bound Vortex-antivortex pairs
Disordered state
Exponential decay of correlation functions
Free Vortex-antivortex
Berezinskii-Kosterlitz-Thouless (BKT) transition
Mermin-Wagner Theorem (1966): In systems with continuous symmetry (e.g., Heisenberg or XY models) and dimensions d ≤ 2, long-range magnetic order is suppressed at finite temperatures due to strong thermal fluctuations.
Topological BKT transition: Occurs in 2D systems with continuous symmetry (Such as 2D XY systems, 2D superfluids, thin superconducting films)
C(r) ∼ r−η(T) with 0 < η(T) < ¼ (T < TBKT)
​
C(r) ∼ e−r/ξ(T) (T > TBKT)
Correlation functions
Above TBKT
Below TBKT

## Slide 3
Short and long-range magnetic ordering and emergent topological transition in (Mn1-xNix)2P2S6
X | TBKT (K) | TN (K) | TS (K)
0 | 24 | 80 | 150
0.3 | 20 | 60 | 140
0.7 | 40 | 70 | 170
1 | 60 | 153 | 
System | TBKT (K) | b
X=0.7 | 31 | 1.04
X=0.3 | 22 | 1.39
Spin-spin correlation length